DURASTIC S405 EPOXY SURFACING

DURASTIC S405 EPOXY SURFACING is a two part, solvent free, coloured epoxy coating. It may be used direct to the deck or as a functional and decorative finish to Durastic underlays. It is available as a smooth finish or with varying degrees of anti-slip. It can be supplied in red, green, grey, blue, beige and buttermilk.

WHERE LAID

In all areas where an impervious coating is required with or without an anti-slip finish.  Ideal in all wet spaces such as galleys, wet changing rooms, internal working alleyways, machine shops, car decks, ramps, weatherdecks (not on the crowns of crew and passenger accommodation where deckhead insulation is not fitted).

TECHNICAL DATA

DENSITY:

1,480 Kg per m3.

LAID THICKNESS:

0.5 mm in two coats

TENSILE STRENGTH:

150 x 150 x 2 mm Sheet

4.1 N/mm².

COMPRESSIVE STRENGTH:

40 x 40 x 75mm Blocks 42N/mm².

FLEXURAL STRENGTH:

A sample on 600 x 100 x 0.9mm steel will bend over an arc of 900mm radius without cracking or detachment.

HARDNESS:

Using Vickers Pyramid Hardness Tester Load 20g.  153 V.PH

RESISTANCE TO ABRASION:

Using R.E.L. Abrasion Apparatus 2000 cycles at 1000g. loading gives weight loss 0.05%.

SURFACE PREPARATION

DURASTIC UNDERLAYS

Cementitious underlays should be properly cured with a moisture content of less than 6%.

S450 epoxy underlay can be overlaid after 24 hours.  All underlays must be clean, free of oil, grease, dirt etc.

STEEL

Steel deck plates must be free from oil, grease, dirt, rust, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the S405.

A proprietary degreaser should be used.  The steel should be mechanically wire brushed to remove dirt, rust etc., paying particular attention along plate welds and boundary edges.

A mechanical discing machine using 7 inch No. 16 grit (Coarse) discs can be used on heavier deposits.

On older steel in poor condition with a heavier build up of old paint and, perhaps, pitted areas of corrosion it may be necessary to shot blast.  In all cases once the steel has been cleaned and roughened the S405 should be applied as soon as possible before any further rust develops.

ALUMINIUM

Aluminium deck plates must be free from oil, grease, dirt, loose paint etc.

It is essential that all traces of grease and oil are removed before application of the S405.

A proprietary degreaser should be used.

The aluminium should be lightly abraded with a medium grit disc to provide a physical key.

SHOP PRIMERS

Because of the diversity of shop primers for steel it is impossible to give compatibility information for our systems with each specific primer in this short section.

However we can say that Durastic Systems can be applied over a wide range of primers.  In particular the popular rapid curing thin coat two-pack primers are suitable.

Primers containing zinc pigments such as silicates or phosphates usually have tie coats applied to prevent salt formation which makes them suitable.

Normally on a “new build” by the time the deck is released for underlay application the primer is almost walked off.  The installer should have checked that tie-coats had been applied if necessary and then the deck should be prepared by degreasing and removing dirt etc. with a wire brush as detailed in the steel preparation section.

We must stress that if there are any doubts about the type of paint we would much prefer that the installer tell us what primer is on the deck and we will establish with the paint manufacturer the type of paint system before deciding on its compatibility.

COVERAGE

- S405 Epoxy Resin        1 x 3.2 Kg tub

- S405 Epoxy Hardener  1 x 0.8 Kg tub

- covers 10m² on a smooth surface

OPERATIONAL PROCEDURE

- Remove all rust, dirt etc.

- Apply roller / brush coat of S405 Epoxy Top Coat.

- Sprinkle anti-slip grit and leave overnight.

- Apply second roller / brush coat of S405 Top Coat.

- Allow to cure for 24 hours.

MIXING AND APPLICATION

Mix contents of the two tubs (resin and hardener) together using a stirrer paddle and drill until thoroughly dispersed.  Pour a quantity of the material into a paint tray and apply a coat of S405 Epoxy top coat over the substrate.  Boundary and around fittings may be finished with a brush.

Note: If an anti-slip finish is required then the anti-slip grit may be incorporated in this first coat by mixing the anti-slip grit into the S405 Epoxy top coat whilst it is in the paint tray or by sprinkling the anti-slip grit onto the surface of the first coat whilst it is still wet (i.e. within 30 minutes).  Allow to set overnight and apply a second coat of S405 Epoxy top coat.  The S405 Epoxy top coat must be allowed to cure for 24 hours before being subjected to trafficking.

TEMPERATURE

Ideally the ambient temperature should be 15°C - 25°C when mixing and laying.  S405 should not be laid below 10°C as curing will be noticeably retarded and the resin will be stiffer to use and spread.

STORAGE AND SHELF-LIFE

Epoxy resin and hardener can be stored in temperatures between 5°C to 35°C.  The materials can be stored for 2 years when the above conditions prevail.

CERTIFICATES AND APPROVALS

All materials are manufactured and tested using our Quality Management System which has been approved by Lloyds Register Quality Assurance Limited to 1S0 9001 : 2008.

HEALTH AND SAFETY

Normal precautions to avoid getting the epoxy resin and hardener onto the skin or eyes should be observed, safety gloves, overalls and goggles should be worn when handling epoxy systems.

Detailed Material Safety Data Sheets and C.O.S.H.H. Assessments are available for safe working with the product.  These should be consulted before commencing work to ensure safe working practice.

TECHNICAL ADVICE

This Data Sheet, although comprehensive, cannot cover every possible application. Our Technical Department + 44 (0) 191 4832299 will be pleased to advise on specific applications.IF IN DOUBT - ASK!